Supporting Information

Selective capture of iodate anions by a cerium-based metal-organic framework

Yuting Zhao1,#, Jie Li1,#, Long Chen1,#, Qi Guo1, Lingyi Li1, Linwei He1, Fuwan Zhai1, Mingxing Zhang1, Zhifang Chai1 & Shuao Wang1,*

1State Key Laboratory of Radiation Medicine and Protection, School of Radiation Medicine and Protection, Collaborative Innovation Center of Radiological Medicine of Jiangsu Higher Education Institutions, Soochow University, Suzhou 215123, China

#Contributed equally to this work.

*Corresponding authors (email: shuaowang@suda.edu.cn)

Scheme S1  Schematic representation of the synthesis of Ce(IV)-MOF-808 by the solvothermal method.

Figure S1  The powder of Ce(IV)-MOF-808.

Figure S2  Zeta potential of Ce(IV)-MOF-808.

Figure S3  A picture showing the color changes of IO3- conversion to I3- during the adsorption kinetics (pH=7).

Figure S4  A picture showing the color changes of IO3- conversion to I3- during the adsorption kinetics (pH=2).

Figure S5  UV spectra of IO3- solution during removal with Ce(IV)-MOF-808 (pH=7: (a), (b); pH=2: (c), (d)).

Figure S6  Pseudo-first-order kinetic model (pH=7: (a); pH=2: (c)) and pseudo-second-order kinetic model (pH=7: (b); pH=2: (d)) of IO3-.

Figure S7  FT-IR spectrum (a) and PXRD pattern (b) of Ce(IV)-MOF-808 before and after β irradiation.

Figure S8  Photograph of the auto solid-phase extraction system (SepathsUP4).

Figure S9  SEM-EDS of Ce(IV)-MOF-808 (a, d), Ce(IV)-MOF-808_IO3- (pH=7) (b, e), and Ce(IV)-MOF-808_IO3- (pH=2) (c, f).

Figure 10  SEM-EDS mapping of Ce(IV)-MOF-808 (a), Ce(IV)-MOF-808_IO3- (pH=7) (b), and Ce(IV)-MOF-808_IO3- (pH=7) (c).

Figure S11  FT-IR spectra of Ce(IV)-MOF-808 before and after adsorption.

Table S1  Composition of anions in the Hanford groundwater (HGW) (obtained from the Hanford Groundwater Monitoring Report) [1].

| Anion | Concentration (mg·L-1) |
| --- | --- |
| Cl- | 30.09 |
| NO3- | 46.5 |
| SO42- | 96 |
| CO32- | 120 |
| IO3- | 1 |

Table S2  Composition of anions in the Beishan groundwater (BGW) [2].

| Anion | Concentration (mg·L-1) |
| --- | --- |
| Cl- | 1261.33 |
| NO3- | 27.10 |
| SO42- | 1259.67 |
| HCO3- | 96.37 |
| IO3- | 1 |

Table S3  Fitting results and parameters of Ce(IV)-MOF-808 based on the pseudo-first-order and pseudo-second-order models.

| Solution | Pseudo-first-order |  |  | Pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | k1 (min-1) | qe (mg·g-1) | R2 | k2 (g·mg-1·min-1) | qe (mg·g-1) | R2 |
| IO3- (pH = 7) | 1.09×10-2 | 6.53 | 0.69 | 0.01 | 48.69 | >0.99 |
| IO3- (pH = 2) | 1.14×10-2 | 9.48 | 0.83 | 0.01 | 51.47 | >0.99 |

Table S4  Comparison of the distribution coefficient (Kd) of Ce(IV)-MOF-808 (this work) and other reported materials for IO3-.

| Material | Solid/liquid ratio (g·L-1) | Kd (mL·g-1) | Ref |
| --- | --- | --- | --- |
| HBHal | 5 | 131.60 | [3] |
| Cu2O@CH | 3 | 5.33×102 | [4] |
| NiAl LDH | 10 | 1.69×103 | [5] |
| CoAl LDH | 10 | 2.13×103 | [5] |
| ZrSbO2 | 2 | 1.00×104 | [6] |
| ZrO2 | 2 | 1.00×104 | [6] |
| CeO2 | 5 | 4.50×101 | [7] |
| Bi-Form | 5 | 1.54×104 | [7] |
| FeH | 5 | 8.39×104 | [7] |
| ASM-125 | 5 | 1.14×105 | [7] |
| ASM-10-HP | 5 | 8.57×105 | [7] |
| CHM-20 | 5 | 1.27×106 | [7] |
| Ce(IV)-MOF-808 | 1 | 2.60×106 | This work |

Table S5  Fitting results and parameters of Ce(IV)-MOF-808 based on the Freundlich and Langmuir models.

| Solution | Freundlich |  |  | Langmuir |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | KF ((mg·g-1) × (L1/n·mg-1/n)) | n | R2 | qm (mg·g-1) | KL (L·mg-1) | R2 |
| IO3- (pH = 7) | 56.08 | 3.19 | 0.95 | 361 | 3.7×10-2 | >0.99 |
| IO3- (pH = 2) | 101.57 | 2.94 | 0.90 | 623 | 8.4×10-2 | >0.99 |

Table S6  Comparison of adsorption parameters by Ce(IV)-MOF-808 (this work) and other reported materials for IO3-.

| Material type | Material | Solid/liquid ratio (g·L-1) | pH | Equilibration time (min) | qm (mg·g-1) | Ref |
| --- | --- | --- | --- | --- | --- | --- |
| Oxides/composites | ZrSbO2 | 2 | 4.7 | 60 | 612.5 | [6] |
|  | ZrO2 | 2 | 4.3 | 60 | 560 | [6] |
|  | Cu2O@CH | 1 | 6 | 30 | 313.4 | [4] |
|  | Bi2O2.33 | 0.2 | 7 | 20 | 228.8 | [8] |
|  | δ-Bi2O3@PES | 1 | - | 300 | 170.6 | [9] |
| Natural material | Dried duckweed powder | 4 | 7 | 5760 | 5.1 | [10] |
|  | DNTD | 8 | - | 1440 | 3.3 | [11] |
|  | Pomelo peel | 2 | - | 5760 | 3.3 | [12] |
| Resin | Purolite A530E | 1 | 7 | 90 | 53.3 | [13] |
| Naturally occurring porous minerals | HDPy-bent | 2 | 4.3 | 10 | 50.2 | [14] |
|  | HBHal | 5 | 6.4 | 2880 | 3.9 | [3] |
| LDHs | NiAl LDH | 5 | 5.8-6.4 | 20 | 395.5 | [5] |
|  | CoAl LDH | 5 | 5.8-6.4 | 20 | 378.1 | [5] |
|  | CoCr-4NC LDH | 1 | 5.9 | 60 | 363.0 | [15] |
|  | Mg2-Al-NO3 LDH | 0.75 | - | 240 | 154.2 | [16] |
| MOFs | MOF-808 | 0.25 | - | 2880 | 233 | [17] |
|  | Ce(IV)-MOF-808 | 1 | 2 | 60 | 623 | This work |

Table S7  Results of IO3- removal by Ce(IV)-MOF-808 from simulated nuclear wastes.

| Simulated waste | Solid-to-liquid ratio (g·L-1) | Removal percentage |
| --- | --- | --- |
| Hanford groundwater (HGW) | 1 | 24.16 |
|  | 5 | >99% |
| Beishan groundwater (BGW) | 1 | 45.93 |
|  | 5 | >99% |

References

1	Levitskaia TG, Campbell EL, Hall GB, et al. Characterization of spent Purolite A530E resin with implications for long-term radioactive contaminant removal. J Environ Chem Eng 2020; 8: 104155.

2	Zheng M, Zhang QC, Huang YL, et al. Determination of Representative Ground-water for Corrosion Assessment of Candidate Materials Used in Beishan Area Preselected for High-level Radioactive Waste Disposal Repository. J Chinese Soc Corros Prot 2016; 36: 185-190.

3	Yu WB, Xu HF, Tan DY, et al. Adsorption of iodate on nanosized tubular halloysite. Appl Clay Sci 2020; 184: 105407.

4	Yan CH, Li JY, Tan C, et al. Cuprous Oxide-Based Cationic Hydrogel by the Integration of Enrichment and Immobilization of Radioiodine (I-, IO3-) in Aqueous Solution. ACS Appl Mater Interfaces 2023; 15: 28135-28148.

5	Kang J, Cintron-Colon F, Kim H, et al. Removal of iodine (I- and IO3-) from aqueous solutions using CoAl and NiAl layered double hydroxides. Chem Eng J 2022; 430: 132788.

6	Suorsa V, Otaki M, Virkanen J, et al. Pure and Sb-doped ZrO2 for removal of IO3- from radioactive waste solutions. Int J Environ Sci Technol 2022; 19: 5155-5166.

7	Cordova EA, Garayburu-Caruso V, Pearce CI, et al. Hybrid Sorbents for 129I Capture from Contaminated Groundwater. ACS Appl Mater Interfaces 2020; 12: 26113-26126.

8	Liu SW, Kang SH, Wang HM, et al. Nanosheets-built flowerlike micro/nanostructured Bi2O2.33 and its highly efficient iodine removal performances. Chem Eng J 2016; 289: 219-230.

9	Zhao Q, Chen GY, Wang ZR, et al. Efficient removal and immobilization of radioactive iodide and iodate from aqueous solutions by bismuth-based composite beads. Chem Eng J 2021; 426: 131629.

10	Zhang K, Chen T. Sorption and removal of iodate from aqueous solution using dried duckweed (Landoltia punctata) powder. J Radioanal Nucl Chem 2018; 316: 543-551.

11	Liu P, Chen T, Zheng JG. Removal of iodate from aqueous solution using diatomite/nano titanium dioxide composite as adsorbent. J Radioanal Nucl Chem 2020; 324: 1179-1188.

12	Da TX, Chen T. Optimization of experimental factors on iodate adsorption: a case study of pomelo peel. J Radioanal Nucl Chem 2020; 326: 511-523.

13	Zhao YT, Li J, Chen L, et al. Efficient removal of iodide/iodate from aqueous solutions by Purolite A530E resin. J Radioanal Nucl Chem 2023; 332: 1193-1202.

14	Yang JQ, Tai WY, Wu F, et al. Enhanced removal of radioactive iodine anions from wastewater using modified bentonite: Experimental and theoretical study. Chemosphere 2022; 292: 133401.

15	Kang J, Levitskaia TG, Park S, et al. Nanostructured MgFe and CoCr layered double hydroxides for removal and sequestration of iodine anions. Chem Eng J 2020; 380: 122408.

16	Zhang D, Liu XY, Zhao HT, et al. Application of hydrotalcite in soil immobilization of iodate (IO3-). RSC Adv 2018; 8: 21084-21091.

17	Copeman C, Bicalho HA, Terban MW, et al. Adsorptive removal of iodate oxyanions from water using a Zr-based metal-organic framework. Chem Commun 2023; 59: 3071-3074.