SUPPORTING INFORMATION

Ultrafast and stable flash memory with metal nanocrystals for logic-in-memory computing

Chuhang Li1, Yang Wang1,2*, Yongbo Jiang1, Shuiyuan Wang1, Chunsen Liu1,2*, and Peng Zhou1,2*

1 State Key Laboratory of Integrated Chips and Systems, College of Integrated Circuits and Micro-Nano Electronics, Frontier Institute of Chip and System, Zhangjiang Fudan International Innovation Center, Fudan University, Shanghai 200433, China.

2 Shaoxin Laboratory, Shaoxing 312035, China.

*Email: chunsen_liu@fudan.edu.cn; yang_wang@fudan.edu.cn; pengzhou@fudan.edu.cn

Figure S1. The SEM images of Pt nanocrystals formed by different conditions. Initial thickness of thin metal layer and RTA temperature are two significant factors on the formation of Pt nanocrystals. For films thinner than 0.5 nm nanocrystals are observable even without the post-RTA processing. As the film thickness increases, the deposited film evolves from isolated nanocrystals to irregular interlocked islands. After RTA, well-defined nanocrystals with distinguishable shape and certain size distribution are obtained.

The bottom gate was patterned by e-beam lithography (EBL) and a 5/15 nm Cr/Pt stack was deposited using e-beam evaporation (EBE) on the silicon substrate with a 100 nm-thick SiO2 thermal oxide film. Lift-off process was conducted through soaking in acetone for 1.5 hours at 75 ℃ and for 3 hours at room temperature to obtain clean bottom gate electrodes. The sample was then annealed in the N2 atmosphere at 200 ℃ for 2.5 hours and subsequent O2 plasma treatment (50 W, 20 s) were performed to further clean and activate the surface for dielectric deposition. A 15 nm-thick HfO2 blocking oxide was deposited by thermal atomic layer deposition (ALD) at 150 ℃ followed by annealing in O2 at 200 ℃ for 1 hour to fill the oxygen vacancies in the dielectric. The floating gate was patterned by EBL and 0.5 nm Pt was then deposited by EBE. After the lift-off process the thin metal film was converted to Pt nanocrystals by the rapid thermal annealing (RTA) process at 400 ℃ for 20 s. h-BN bulk crystals and CVD monolayer MoS2 film were purchased from HQ Graphene and SIX CARBON TECH, respectively. h-BN flake was transferred onto the floating gate by the dry-transfer approach and annealed in N2 atmosphere at 200 ℃ for 2.5 hours to remove tape residues and enhance adhesion to the substrate. CVD MoS2 was transferred onto h-BN by a polystyrene (PS)-assisted transfer process and soaked in toluene over 12 hours to remove the PS supporting layer. The sample was again annealed in N2 atmosphere at 200 ℃ for 2.5 hours. Next, MoS2 channels were defined by EBL with a negative photoresist process (MAN 2403) and etched into strips by O2 plasma. The sample was soaked in NMP at room temperature overnight to remove photoresist. Finally, the source and drain electrodes were defined by EBL followed by depositing Cr/Au (5nm/40nm) using EBE.

Figure S2. The fabrication process of the nonvolatile flash memory.

Figure S3. AFM characterization of the back gate. Edge burrs are absent, and no detectable nanoparticles or residues are observed across the entire device area. Clean and flat surfaces are confirmed, which enhances the quality of the blocking layer and mitigates the risk of dielectric breakdown. By minimizing electrode surface roughness, dielectric disorder on the tunneling layer's surface is suppressed, thereby improving device performance.

Figure S4. The transfer curves of HfO2 dielectric transistors before and after annealing in O2. The threshold voltages shift towards positive directions, indicating the passivation of oxygen vacancies in the HfO2 dielectric.

Figure S5. AFM image of the nonvolatile flash memory. The thickness of h-BN tunneling layer is determined to be around 11.5 nm.

Figure S6. Gate leakage current versus back gate voltage of the nonvolatile flash memory.

Figure S7. Electrical characteristics of the MoS2/h-BN FET. (a) Optical image of the device which does not have Pt nanocrystals floating gate. (b) Transfer characteristic curves of the MoS2/h-BN heterostructure. (c) A plot of the transfer curve within ±10 V in linear coordinates. No memory window is observed.

Figure S8. The waveform of the ultrafast voltage pulses. The voltage pulses generated by the SPGU in the B1500 were captured and characterized by the oscilloscope.

Figure S9. Energy band diagram of the floating gate memory under flat biases, which corresponds to steady states. W designates for the work function, Eg represents the band gap and X stands for the electron affinity.

Figure S10. The electrical characteristics of the nonvolatile flash memory after operations of 50000 endurance cycles. Vds value is always 100 mV. (a) Transfer curve shows normal transistor performance. (b) Gate leakage current as a function of back gate voltage. The small leakage current demonstrates that the blocking layer preserves device functionality under repeated electrical stresses without significant degradation in device operation. (c) Time traces of the channel current upon applying +22 V / -24 V pulses with a duration of 50 ns. The transient change of the current indicates the breakdown of the tunneling layer. The electrons cannot be obstructed by the h-BN layer and retained in the floating gate anymore and the memory becomes volatile.

Figure S11. Retention performance of continuous Pt floating gate memory device. VDS value is always 0.1 V. (a) Schematic structure diagram of continuous Pt floating gate memory device. (b) Transfer characteristic curves of the flash memory at a different time interval. The device was reset to state 1 and programed to state 0 by a 12 V, 50 ns pulse. (c) Transfer characteristic curves of the flash memory at a different time interval. The device was reset to state 0 and erased to state 1 by a -13 V, 50 ns pulse. The threshold voltage will quickly return towards the initial value and the memory device has limited retention properties, which hinders its nonvolatile potential.

Figure S12. Time dependence of multilevel states. The channel current was read at Vds = 0.1 V and Vgs = 0 V. A sequence of incremental voltage pulses starting from -19 V with an increment of 1 V were each applied for a duration of 50 ns to achieve more than 8 distinct storage states.

Figure S13. The fabrication process of the logic-in-memory circuits.

Table S1. Comparisons of floating gate transistors based on 2D materials.

| device structure | operational speed | retention | endurance | on/off ratio | reference |
| --- | --- | --- | --- | --- | --- |
| MoS2/h-BN/MLG/SiO2/Si | 100 µs | 1500 s | - | 103 | 1 |
| InSe(MoS2)/h-BN/MLG/SiO2/Si | 21 ns | 5400 s | 2000 cycles | 1010 | 2 |
| MoS2/h-BN/MLG/SiO2/Si | 20 ns | 5300 s | 1390 cycles | 106 | 3 |
| MoS2/HfO2/Pt/HfO2/Pt | 20 ns | 1000 s | - | 105 | 4 |
| ReS2/h-BN/MLG/SiO2/Si | 30 ns | 1100 s | 1000 cycles | 107 | 5 |
| MoS2/HfO2/Pt/HfO2/Pd | 10 ms | 3600 s | 5000 cycles | 106 | 6 |
| Cr/HfOx/HfS2/HfOx/MoS2/SiO2/Si | 1 ms | 105 s | 1000 cycles | 107 | 7 |
| Cr/Al2O3/Au NPs/pV3D3/MoS2 | 10 ms | 105 s | 10000 cycles | 105 | 8 |
| MoS2/HfO2/Pt/HfO2/Pt | 100 ms | 3600 s | 500 cycles | 106 | 9 |
| MoS2/HfO2/Pt/HfO2/Pt | 1 ms | 18000 s | 5000 cycles | 104 | 10 |
| MoS2/Al2O3/Pt/Al2O3/Cr | 5 µs | 10000 s | 105 cycles | 107 | 11 |
| MoS2/h-BN/PdSe2/SiO2/Si | 40 ns | 10000 s | 1000 cycles | 107 | 12 |
| MoS2/h-BN/Te/SiO2/Si | 100 ns | 4000 s | 4000 cycles | 108 | 13 |
| ReS2/h-BN/Te/SiO2/Si | 10 ms | 10000 s | 1000 cycles | 106 | 14 |
| MoS2/h-BN/Pt NPs/HfO2/Pt | 20 ns | 100000 s | 20000 cycles | 106 | This work |

Notes: MLG: multilayer graphene; pV3D3: poly(1,3,5-trimethyl-1,3,5-trivinyl cy

clotrisiloxane); NPs: nanoparticles.

Table S1 shows a comprehensive performance comparison with previous works on 2D floating gate transistors. Our flash devices operate at an ultrafast speed of 20 ns and exhibit a large on/off ratio of 106. The program and erase states can be stably maintained for more than 105 s and the device can be switched back and forth between states 0 and 1 up to 20000 cycles without obvious degradation.

References

(1)	Sup Choi M, Lee GH, Yu YJ, Lee DY, Hwan Lee S, Kim P, Hone J, Jong Yoo W. Controlled Charge Trapping by Molybdenum Disulphide and Graphene in Ultrathin Heterostructured Memory Devices. Nat Commun 2013; 4.

(2)	Wu L, Wang A, Shi J, Yan J, Zhou Z, Bian C, Ma J, Ma R, Liu H, Chen J, Huang Y, Zhou W, Bao L, Ouyang M, Pennycook SJ, Pantelides ST, Gao HJ. Atomically Sharp Interface Enabled Ultrahigh-Speed Non-Volatile Memory Devices. Nat Nanotechnol 2021; 16: 882–887.

(3)	Liu L, Liu C, Jiang L, Li J, Ding Y, Wang S, Jiang YG, Sun YB, Wang J, Chen S, Zhang DW, Zhou P. Ultrafast Non-Volatile Flash Memory Based on van Der Waals Heterostructures. Nat Nanotechnol 2021; 16: 874–881.

(4)	Jiang Y, Liu C, Cao Z, Li C, Liu Z, Wang C, Xiang Y, Zhou P. A Scalable Integration Process for Ultrafast Two-Dimensional Flash Memory. Nat Electron 2024; 7: 868–875.

(5)	Lu H, Wang Y, Han X, Liu J. An Ultrafast Multibit Memory Based on the ReS2/h-BN/Graphene Heterostructure. ACS Nano 2024; 18: 23403–23411.

(6)	Migliato Marega G, Zhao Y, Avsar A, Wang Z, Tripathi M, Radenovic A, Kis A. Logic-in-Memory Based on an Atomically Thin Semiconductor. Nature 2020; 587: 72–77.

(7)	Niu W, Zou X, Tang L, Bu T, Zhang S, Jiang B, Dang M, Hong X, Ma C, He P, Zhou P, Liu X, Liao L. Van Der Waals Gap Enabled Robust Retention of MoS2 Floating‐gate Memory for Logic‐in‐memory Operations. Adv Funct Mater 2025; 35.

(8)	Kim YK, Park S, Choi J, Park H, Jang BC. Low‐power Charge Trap Flash Memory with MoS2 Channel for High‐density In‐memory Computing. Adv Funct Mater 2024; 34: 2405670.

(9)	Migliato Marega G, Ji H. G, Wang Z, Pasquale G, Tripathi M, Radenovic A, Kis A. A Large-Scale Integrated Vector–Matrix Multiplication Processor Based on Monolayer Molybdenum Disulfide Memories. Nat Electron 2023; 6: 991–998.

(10)	Migliato Marega G, Wang Z, Paliy M, Giusi G, Strangio S, Castiglione F, Callegari C, Tripathi M, Radenovic A, Iannaccone G, Kis A. Low-Power Artificial Neural Network Perceptron Based on Monolayer MoS2. ACS Nano 2022; 16: 3684–3694.

(11)	Cai Y, Yang J, Hou Y, Wang F, Yin L, Li S, Wang Y, Yan T, Yan S, Zhan X. 8-Bit States in 2D Floating-Gate Memories Using Gate-Injection Mode for Large-Scale Convolutional Neural Networks. Nat Commun 2025; 16: 2649.

(12)	Wang W, Jin J, Wang Y, Wei Z, Xu Y, Peng Z, Liu H, Wang Y, You J, Impundu J, Zheng Q, Li YJ, Sun L. High‐speed Optoelectronic Nonvolatile Memory Based on van Der Waals Heterostructures. Small 2023; 19.

(13)	Zha J, Xia Y, Shi S, Huang H, Li S, Qian C, Wang H, Yang P, Zhang Z, Meng Y, Wang W, Yang Z, Yu H, Ho JC, Wang Z, Tan C. A 2D Heterostructure‐based Multifunctional Floating Gate Memory Device for Multimodal Reservoir Computing. Adv Mater 2024; 36: 2308502.

(14)	Bach TPA, Cho S, Kim H, Nguyen DA, Im H. 2D van Der Waals Heterostructure with Tellurene Floating-Gate for Wide Range and Multi-Bit Optoelectronic Memory. ACS Nano 2024; 18: 4131–4139.